- 产品名称：3S低温水溶纤维

I. Name of product: 3S Low Temperature Water Soluble Fiber

二、性能概述

低温水溶纤维是以PVA为原料，采用凝胶纺丝技术制得。特性为:

1、水溶温度低，可在20～60℃水中完全溶解而没有残留物；芒硝法只能生产80℃以上的较高温度的普通水溶纤维。

2、纤维强度较高，纤维截面呈圆形，尺寸稳定性较好，线密度、伸度适中，适合纺织加工要求。

3、耐虫蛀霉菌性能良好；耐光性好，在长时间的日照下，纤维强度损失率大大低于其它纤维。

4、纤维中不含芒硝,纺织加工时无芒硝粉尘，对人体和环境无毒无害。

II. Performance overview

The low-temperature water-soluble fiber is taken PVA as raw material and adopted a gel spinning technique with the following features:

1. Low water soluble temperature. It leaves no residue when dissolves in water at 20-60 ℃. The Sodium sulfide method can only produce ordinary fibers soluble in a high temperature of 80 ° C or higher.

2. Suitable for textile processing due to its high fiber strength, round fiber cross section, good dimensional stability, moderate linear density and the elongation.

3. Good resistance to insects and mildew, good resistance to light, much lower strength loss than other fibers on long exposure to sunlight.

4. Non-toxic and harmless to human and environment. The absence of sodium sulfide leads to free dust hazard during spinning process.

三、特性指标

1、溶解温度（℃） T±5 （注：T随用户、生产要求而定，普通情况为20℃、40℃、60℃, 70℃）

2、单纤线密度（dtex） M（1±0.10）（注：M随用户、生产要求而定，普通情况为1.40dtex、1.56dtex、1.67dtex、2.20dtex）

3、干断裂强度 （cN/dtex）≥ 4.5

4、干断裂伸度（％） 14±3

5、长度 （mm） L±2.0 （注：L随用户要求而定，普通情况为38mm、51mm、76mm）

6、卷曲数 （个/25mm） ≥ 4.5

7、含油率 ％ 0.20～0.60

III. Specification

1. Dissolve temperature (°C) T±5 (T can be customized at 20℃、40℃、60℃, 70℃)

2. Single fiber linear density (dtex) M (1 ± 0.10) (M can be customized at 1.40dtex、1.56dtex、1.67dtex、2.20dtex)

3. Dry breaking strength (cN/dtex) ≥ 4.5

4. Dry fracture elongation (%) 14 ± 3

5. Length (mm) L ± 2.0 (L can be customized at 38mm、51mm、76mm)

6. Number of crimp (number / 25mm) ≥ 4.5

7. Sizing agent content, 0.2-0.6%

四、应用领域

1、水溶纱线。用于生产无捻毛巾、无捻针织内衣、遇水收缩水绒套、收缩衣、洗衣袋用的缝纫线、水溶纱复合包装袋等。

2、水溶无纺布。作为绣花的骨架材料（刺绣基布），可单独在上面绣花，也可与其它服装面料衬在一起使用，绣完花型之后只要在热水中处理掉水溶无纺布，即可保留绣制的花型。另外可作为一次性防尘外衣、揩布、医疗、卫生、包装及旅游制品等。

3、混纺。与毛、麻、棉、羊绒等混纺，可增加纱线强度，提高可纺性、织造性。在染整前将混纺织物中的水溶纤维溶解除去，可得到蓬松、轻量、柔软、透气等性能良好的织物，从而提高了产品档次，增加了产品附加价值。

IV. Application

1. Water soluble yarn. It is used in the production of twistless towels, twistless knitted underwear, water shrinkable velvet sleeves, shrink garments, sewing threads for laundry bags, water-soluble yarn composite packaging bags, etc.

2. Water-soluble non-woven fabric. As the embroidered skeleton material (embroidery base fabric), it can be embroidered on the top, or it can be used together with other fabrics. After embroidering the pattern, just put the fabric into the hot water to remove the water-soluble non-woven fabric, the embroidered flower is retained. It can also be used as a dustproof outerwear, crepe cloth, medical, sanitary, packaging and travelling products.

3. Blended spinning. Blended with wool, hemp, cotton, cashmere, etc., which can increase the yarn strength and improve the spinnability and weavability. The water-soluble fiber in the blended fabric is dissolved and removed before dyeing, and a fabric with good properties such as fluffiness, light weight, softness, and gas permeability can be obtained, thereby upgrading the product and adding value to the product.